 
APPENDIX A:
PHOTOGRAPHS TAKEN DURING JIV AT 10’’ CLOUGH CREEK/TEBIDABA PIPELINE AT AZAGBENE IN EKEREMOR LOCAL GOVERNMENT AREA OF BAYELSA STATE.
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PIPELINE WRAP NOT TEMPERED
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                        BEFORE EXCAVATION				            AFFER EXCAVATION (SPILL POINT)	
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 UNWRAPPING THE PIPELINE FOR SPILLED POINT	                     SPILL POINT (Corrosion)
 ASSESSMENT BY THE REPAIR PERSONNEL		 

 (
UTM RESULT
AROUND LEAK
i
. 3.5mm
ii
. 3.9mm
iii
. 3.5mm
iv
. 3.9mm
PIPELINE SCHEDULE
MAX: 12.70mm
MIN: 9.70mm
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UTM (Uitrasonic thickness measurement)		          READING WITHIN AND AROUND THE LEAK POINT  
 MACHINE   						          USING UTM BY NAOC PERSONNEL 
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                      	IMPACTED AREA            				                 REPAIR POINT
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